DESCRIPTION

Restoration Shop

AU- Acrylic Urethane Single Stage

AU Acrylic Urethane Single Stage is formulated to give outstanding gloss, depth, chemical resistance and durability in an easy-to-use system.

COMPONENTS

- AU  - Polyurethane Enamel Color

- AU4001 - Polyurethane Hardener

- UR 60 - Urethane Reducer Fast

- UR 70 - Urethane Reducer Medium

- UR 85 - Urethane Reducer Slow

- XR70	 - Exempt Reducer

POT LIFE @ 77°F

2 ½-3 hours

MIXING RATIO

Mixing Ratios:  4 : 1 : 1    4 parts AU Color – 1 part AU4001 Hardener – 1 part UR Reducer (Select for best Temperature). AU Kit contains the exact amount required to obtain the 4 : 1 : 1 Mix Ratio. AU Kit includes 1 Gallon AU Color, 1 Quart AU4001 Hardener and 1 Quart of the Reducer of your choice.

CLEAN UP

KT912 (Check local regulations)

SUBSTRATES

AU Series Acrylic Urethane may be applied over: Cleaned, sanded and primed OEM or Refinish topcoat. Kustom Shop KEP Epoxy Primer / Sealer. Kustom Shop KUP Urethane Primer. Kustom Shop KFP Hi-Build 2K Primer Surfacer Kustom Shop KPP Polyester Primer, Kustom Shop KL611 Old school Acrylic Lacquer Primer.

- Epoxy Primer

- Properly Prepared OEM Surface

- Properly Prepared Aluminum and Steel.

SURFACE PREPARATION

USE RECOMMENDED UNDERCOAT SYSTEM FOLLOWING RECOMMENDED PROCEDURES.

- Wipe with KW901 Grease and Wax Remover or KW902 Anti-Static Panel Kleaner

- Abrade with 150 grit then 320 grit sandpaper or equivalent.

- Wipe again with KW901 Grease and Wax Remover or KW902 Anti-Static Panel Kleaner

- For best results apply anti-corrosive primer such as KEP Series epoxy primers over bare metal.

APPLICATION

For Air Spray

- Spray 2 - 3 medium wet coats or until full hiding is achieved

- Allow 10 -15 minutes @ 70 F flash time between coats

DRY TIMES

AIR DRY @ 77°F

Tack Free	2 Hours

To Tape 	6 Hours

To Recoat	16 Hours

Optional Clear coating: If desired, a clear coat can be applied to provide additional long term durability and wet-look appearance.  KC210 Urethane Speed Clear with KH212 Overall Hardener or KC310 Super Flow Polyurethane Clear with KH311 Hardener. Note: The color must dry a minimum of 4 hours before clear coating.

GUN SETUPS

CONVENTIONAL

Gravity Feed	1.5 mm - 1.8 mm

Siphon Feed	1.6 mm - 1.8 mm

HVLP

Anest Iwata LPH 400	1.4 mm - 1.6 mm

Binks MG1	1.3 mm - 1.6 mm

Devilbiss GTI	1.4 mm - 1.6 mm

Sata 95 & 2000	1.3 mm - 1.5 mm

AIR PRESSURES

CONVENTIONAL @ GUN

Gravity Feed	35 - 45 psi

Siphon Feed	45 - 55 psi

HVLP @ Cap	8 - 10 psi

PHYSICAL DATA

VOC AU Color	3.5 lbs/gal (420 g/l)

VOC AU4001 Hardener	2.6 lbs/gal (312 g/l)

VOC Mixed at 4:1:1 with UR Reducer	4.02 lbs/gal (482 g/l)

VOC Mixed at 4:1:1 with XR70 Reducer	3.32 lbs/gal (398g/l)

Flash Point	46ºF

SAFETY

Before using any Restoration Shop product, be sure to read all MSDS and application instructions and warnings. Always wear a properly fitted air purifying respirator with organic vapor cartridges and particulate filter or a fresh air respirator (depending on product selection), eye protection, gloves and protective clothing during application and until vapors are exhausted. Do not permit anyone without protection in the painting area. This product is intended for use by a professionally trained painter. Keep out of the reach of children.

IMPORTANT: The data on this sheet represent typical values obtained by the methods indicated. Since application variables are a major factor in product performance, this information should serve only as a general guide. Restoration Shop assumes no obligation or liability for use of this information. Unless Restoration Shop agrees otherwise in writing, RESTORATION SHOP MAKES NO WARRANTIES, EXPRESS OR IMPLIED, AND DISCLAIMS ALL IMPLIED WARRANTIES INCLUDING WARRANTIES OF MERCHANTABILITY OR FITNESS FOR A PARTICULAR USE OR FREEDOM FROM PATENT INFRIGNEMENT. RESTORATION SHOP WILL NOT BE LIABLE FOR ANY SPECIAL, INCIDENTAL OR CONSEQUENTIAL DAMAGES.

Unless Restoration Shop agrees otherwise in writing, Restoration Shop’s only obligation for any defect in this product under any warranty that Restoration Shop provides or under any other legal theory will be to replace the defective product, or to refund its purchase price, at Restoration Shop’s option.