DESCRIPTION

Restoration Shop UB – Urethane Basecoat

Restoration Shop UB Basecoat is a state-of-the-art, basecoat/clearcoat system designed to reproduce the hi-tech O.E.M. finishes found on today’s vehicles. It features outstanding coverage, rapid dry time, excellent metallic control and optimum repairability.

COMPONENTS

- UB - High Performance Base Color

- UR 60 - Urethane Reducer Fast

- UR 70 - Urethane Reducer Medium

- UR 85 - Urethane Reducer Slow

POT LIFE @ 77°F

When properly covered at 77°F UB Basecoat will maintain a sprayable viscosity indefinitely

MIXING RATIO

Mixing Ratios:  2 : 1    2 parts UB Color – 1 part UR Reducer.

CLEAN UP

KT912 (Check local regulations)

SUBSTRATES

UB Series Urethane Basecoat may be applied over: Cleaned, sanded and primed OEM or Refinish topcoat. Kustom Shop KEP Epoxy Primer / Sealer. Kustom Shop KUP Urethane Primer. Kustom Shop KFP Hi-Build 2K Primer Surfacer Kustom Shop KPP Polyester Primer, Kustom Shop KL611 Old school Acrylic Lacquer Primer.

- Epoxy Primer

- Properly Prepared OEM Surface

- Properly Prepared Aluminum and Steel.

SURFACE PREPARATION

USE RECOMMENDED UNDERCOAT SYSTEM FOLLOWING RECOMMENDED PROCEDURES.

- Wipe with KW901 Grease and Wax Remover or KW902 Anti-Static Panel Kleaner

- Abrade with 150 grit then 320 grit sandpaper or equivalent.

- Wipe again with KW901 Grease and Wax Remover or KW902 Anti-Static Panel Kleaner

- For best results apply anti-corrosive primer such as KEP Series epoxy primers over bare metal.

APPLICATION

For Air Spray

- Spray 2 - 3 medium-wet coats with an overlap of 50% until full hiding is achieved

- Allow 5-10 minutes @ 70 F flash time between coats

- Dry mils 2.0 to 3.0 mils. Wet mils 4.0 to 6.5 mils.

- Surface temperature should be 50-100°F with less than 80% ambient humidity preferred.

FLASH / DRY TIMES

AIR DRY @ 77°F

Flash Between Coats	5-10 Minutes

To Tape	20-40 Minutes

To Clearcoat	30 Minutes

Note: If the basecoat is allowed to dry more than 24 hours, it must be scuffed and new basecoat applied.

Clear Coating: KC210 Urethane Speed Clear with KH212 Overall Hardener or KC310 Super Flow Polyurethane Clear with KH311 Hardener. Note: The color must dry a minimum of 4 hours before clear coating.

GUN SETUPS

CONVENTIONAL

Gravity Feed	1.3 mm - 1.5 mm

Siphon Feed	1.6 mm - 1.8 mm

HVLP

Anest Iwata LPH 400	1.2 mm - 1.4 mm tip

Binks MG1	1.3 mm - 1.5 mm tip

Devilbiss GTI 	1.4 mm - 1.6 mm tip

Sata 95 & 2000	1.3 mm - 1.5 mm tip

AIR PRESSURES

CONVENTIONAL @ GUN

Gravity Feed 	35 - 40 psi

Siphon Feed	45 - 50 psi

HVLP @ Cap	 8 - 10 psi

PHYSICAL DATA (2:1) Base Color

VOC (Volatile Organic Content)	5.69 lbs/gal (682 g/l)

VOC UR Reducers	7.52 lbs/gal (902 g/l)

VOC X70 Reducers	0.00 Exempt

Flash Point	27°F

SAFETY

Before using any Restoration Shop product, be sure to read all MSDS and application instructions and warnings. Always wear a properly fitted air purifying respirator with organic vapor cartridges and particulate filter or a fresh air respirator (depending on product selection), eye protection, gloves and protective clothing during application and until vapors are exhausted. Do not permit anyone without protection in the painting area. This product is intended for use by a professionally trained painter. Keep out of the reach of children.

IMPORTANT: The data on this sheet represent typical values obtained by the methods indicated. Since application variables are a major factor in product performance, this information should serve only as a general guide. Restoration Shop assumes no obligation or liability for use of this information. Unless Restoration Shop agrees otherwise in writing, RESTORATION SHOP MAKES NO WARRANTIES, EXPRESS OR IMPLIED, AND DISCLAIMS ALL IMPLIED WARRANTIES INCLUDING WARRANTIES OF MERCHANTABILITY OR FITNESS FOR A PARTICULAR USE OR FREEDOM FROM PATENT INFRIGNEMENT. RESTORATION SHOP WILL NOT BE LIABLE FOR ANY SPECIAL, INCIDENTAL OR CONSEQUENTIAL DAMAGES.

Unless Restoration Shop agrees otherwise in writing, Restoration Shop’s only obligation for any defect in this product under any warranty that Restoration Shop provides or under any other legal theory will be to replace the defective product, or to refund its purchase price, at Restoration Shop’s option.